## Slide 1: Net Zero Precast Concrete Factory
`
Musatfa Al-Jalal (CE) – Abdullah Almagabi (CE) – Ali Almaani (CE) – Sadun Alesawi (CE)
Final Target Specifications:
Compressive strength (28d) : 35 MPa
Curing time : 8 hrs
Water permeability : 15-20 cm
Target Area: 3150 m2
Rapid Chloride penetration : 1500-2000 Col
amount of CO2 Captured: 315 kt CO2
Project Statement: Contributing to the Saudi Arabia 2060 vision of achieving net zero by capturing CO2 and storing it in concrete.
Final Prototype
Design Process
Testing
Deliverables:
A Direct air capture unit printed in 3D
A scaled down view of the entire project
Concrete sample injected and cured with CO2.
Constraints:
The machine will not be operating..
It will not show how the process is simulated
Limited budget
Test Results
Introduction
Function of Product
In this Flowchart the team explained the process from capturing CO2 in the atmosphere to storing it in concrete permanently
Area selection:-
DAC functionality & development:-
Capture fraction of 0.9 and an average linear velocity of 8.5, the area required to capture 1 MTCO2/year will be 7500 m2.
Area to Capture the Factory demand.44 m2 or 3150 m2
Factory emissions
CO2 produced by Precast plant + CO2 produced by DAC = CO2 amount should be captured amount.
255kt CO2/year + 60kt CO2/year = 315kt CO2/year
Concrete injection and Curing
CO2 is injected using CarbonCure technology that injects CO2 at a rate of 3.15% per 1 m3 to increase the uptake of CO2 by 12.6%.
Carbonation Curing is done in a curing chamber and concrete will take up to 24% of CO2
****Red line indicates range of targeted specification****
8 Hours | 1 Day | 28 Days
18.6667 | 22.44 | 30
36.88 | 44.5 | 47.4
Rapid Chloride Penetration | 
Sample 1 (Control) | 2221 Col
Sample 2 (Control) | 2255 Col
Sample 3 (Control) | 2374 Col
Sample 4 (CO2 Steam) | 1872 Col
Sample 5 (CO2 Steam) | 1663 Col
Sample 6 (CO2 Steam) | 1576 Col
Control | CO2 Steam
22 mm | 17 mm
24 mm | 14 mm
19 mm | 13 mm
Compressive strength
Water Penetration